## Slide 1
X-ray diffraction
XRD
Røntgendiffraksjon
MENA3100,OBK, 21.04.16
Repetition, exercises and more

## Slide 2
2.4: Wide-angle X-ray diffraction and scattering
Out

## Slide 3
hm ...

## Slide 4
λ ≈ 0.01 to 10 nm
3×1016 Hz to 3×1019 Hz
100 eV to 100 keV
X-rays
Røntgenstråling
(0.1 to 100 Å)
1 eV = 1.6021766208(98)×10−19 J

## Slide 5
(cf. electron microscopes)

## Slide 6
Kα ≈ 0.7 Å
= 18 eV
12.650
13.396
14.166
14.958
15.770
16.615
17.479
18.367
19.279
36 Kr
37 Rb
38 Sr
39 Y
40 Zr
41 Nb
42 Mo
43 Tc
44 Ru
14.113
14.962
15.836
16.737
17.662
18.623
19.608
20.619
21.656
Kβ
Kα

## Slide 7
Wavelength
CuKa1 = 1.54056 Å
CuKa2 = 1.54433 Å
CuKa = 1.5418 Å
I(CuKa1) = 2·I(CuKa2)

## Slide 8
Filters
(cf. EELS)
(cf. ZAF)
Monochromators
(cf. microprobe
(mikrosonde) with WDS)
(And cf. XRD!)

## Slide 9
Bragg’s law
!

## Slide 10
Brief run-through of reciprocal space, Ewald sphere
and intensities first hour next week

## Slide 11
Bragg-Brentano-geometry
Diffractometers

## Slide 12
Diffractogram

## Slide 13
Grazing incidence diffraction
Thin films

## Slide 14
Powder X-ray diffraction
Single crystal diffraction
(énkrystall)

## Slide 15
Random orientation
Powder X-ray diffraction
Bragg-Brentano geometry

## Slide 16
Preferred orientation (foretrukken orientering)

## Slide 17
Why?
Crystallography Open Database

## Slide 18
Indexing

## Slide 20
Extinction
Example: Cubic face centered
Special example: Cubic close packed
Utslukning

## Slide 21
Extinction
Example: Cubic face centered
Special example: Cubic close packed
Utslukning

## Slide 22
But don’t mix up with ...

## Slide 23
Centred lattices gives rice to extinction
Cubic face-centred
Allowed reflexes for fcc:
111, 200, 220, 311, 222, ...
Alle partall eller oddetall
All odd or all even
h + k = 2n, h + l = 2n, k + l = 2n

## Slide 24
Cubic body-centred
110, 200, 211, 220, 310, ...
h + k + l = 2n
Centred lattices gives rice to extinction
Allowed reflexes for bcc:

## Slide 25
Cesiumklorid

## Slide 26
Deformation
Particle size
Scherrer’s equation

## Slide 27
Rietveld refinement
Refinement of atomic positions
Amount of phases